## Slide 1
Philip Humphrey
Adhesive Evaluation Systems, Inc.
Corvallis, Oregon, USA
Experimental Mechanics Sym.
Cambridge, UK July2014
Micro-structural adhesion in
bio-composite materials during
their heated consolidation

## Slide 2: Continuous hot press for wood-based panels
Notes: Our Motivation: Understand mechanisms relevant during consolidation of bio-based materials, ...
... like here in a continuous industrial production.
Prozess kurz beschreiben!
Our interest: Physical processes inside the mat.

## Slide 3
Mechanisms operative during pressing
Predicting internal conditions
The need to optimize adhesion dynamics
The ABES approach
Adhesion in space and time
Implications
What we will discuss

## Slide 4
Hot Platen
Hot Platen
Hot Press
Pressure
Pressure
Heat
GAS
Heat
Notes: There are a lot of mechanisms happening within the mat:
Due to the high temperatures of the pressing platen, heat and moisture is moving towards the center of the mat.
At the same time, the mat is going to be compressed...
… and water vapor and air is escaping through the edges of the mat.
The glue that was given to the particles before cures,…
… and the properties of the mat are changing with time.

## Slide 5: Mechanisms during hot pressing
Thermodynamics
Rheology
Adhesion

## Slide 6: Mechanisms during hot pressing
Thermodynamics
Rheology
Adhesion

## Slide 7: Mechanisms during hot pressing
Thermodynamics
Rheology
C
H
N
O
C
H
N
O
Adhesion

## Slide 8
Mechanisms operative during pressing
Predicting internal conditions
The need to optimize adhesion dynamics
The ABES approach
Adhesion in space and time
Implications
What we will discuss

## Slide 9
University of Hamburg
Adhesive Evaluation Systems
Siempelkamp (Krefeld, Germany)
Project partners:
Simulating the pressing process – a tool

## Slide 10
In-feed section

## Slide 11
Model Boundaries
Notes: Our model boundaries are the surfaces and sides of the mat.
Within the press, the mat-belt interface is assumed to be impermeable to gaseous flow;
… at least so far.
Later on it might be interesting to assume gas injection or removal through the steel belt.
But at the moment gaseous flow is only possible through the mat-atmosphere interface, so through the sides of the mat and through the upper and lower surfaces in front of the press and behind the press.
The lower surface of the mat is assumed to be flat …
… while the thickness of the mat at any position within the press results from the defined press pressure.
Or, if we assume that the press is operated in thickness control mode, the thickness profile can be defined directly.
The curvature of the upper steel belt at the press entrance is variable as well and is defined by the in-feed radius R.

## Slide 12
THERMODYNAMICS
Thermal conductivity fn. mc, density, direction
Gas permeability fn. density, direction
Tortuosity fn. density
Sorptive energy fn. mc, temp., chemistry
RHEOLOGICAL MECHANISMS
Elastic fn. Density, temp., mc
Delayed elastic fn. Density, temp., mc.
Micro-fracture fn. Density, temp., mc.
ADHESION
Strength rate fn. temp., (mc)
Damage rate fn. temp.
Max. strength fn. cure temp. history
Materials properties (input data)
C
H
N
O
C
H
N
O

## Slide 13
Cross-sectional position [mm]
Distance from
press entry [m]
Temperature [°C]
Second densification step
Press outlet
Simulation Results
Temperature

## Slide 14
Width [m]
Gas pressure [kPa]
Distance from press entry [m]
Simulation Results
Gas pressure

## Slide 15
Simulation Results
Density profile

## Slide 16
Mechanisms operative during pressing
Predicting internal conditions
The need to optimize adhesion dynamics
The ABES approach
Adhesion in space and time
Implications
What we will discuss

## Slide 17
The need to optimize adhesion dynamics
  Optimize composite product pressing:
    Minimize pressing time
    Reduce energy consumption
    Control emissions
    Reduce material consumption
    Control product structure – properties
Efficiently design new adhesive formulations
Tailor adhesives to new products and processes

## Slide 18: Mechanisms during hot pressing
Thermodynamics
Rheology
C
H
N
O
C
H
N
O
Adhesion

## Slide 19
Mechanisms operative during pressing
Predicting internal conditions
The need to quantify adhesion dynamics
The ABES approach
Adhesion in space and time
Implications
What we will discuss

## Slide 20: Automated Bonding Evaluation System (ABES)

## Slide 21
The approach
Form small tests bond under controlled conditions
Affect rapid heating to target temperatures
Test strength at various stages of cure
Explore isothermal strength development

## Slide 22
The bond pressing zone

## Slide 23
Bond pulling at controlled rate

## Slide 24
Load measuring @ 2kHz

## Slide 26
Sample cutting and Adhesive micro-spraying

## Slide 27: A typical test bond heating curve (here: for 110°C head setting)
0
40
60
80
100
120
20
20
100
40
80
60
Bond Pressing Time (Sec.)
Glueline Temperature (oC)
Optional Cooling
0

## Slide 28: Bond strength development plot (here: for a UF adhesive, 110°C)
0
2
3
4
5
6
1
100
500
200
400
300
Bond Pressing Time (Sec.)
Shear strength (MPa)
0

## Slide 29: Isothermal bond strength development for a range of temperatures
0
2
3
4
5
6
1
100
500
200
400
300
Bond Pressing Time (Sec.)
Bond strength (MPa)
140oC
125oC
110oC
95oC
0
130oC

## Slide 30: Regressed strength development rate versus temperature
Bond Pressing Temperature (oC)
90 100 110 120 130 140
Isothermal strength
development rates (kPa/sec.)
200
150
100
50
0
strength development rate
temperature
experimentally determined coefficients

## Slide 31: Regressed strength development rate versus temperature
Bond Pressing Temperature (oC)
90 100 110 120 130 140
Isothermal strength
development rates (kPa/sec.)
200
150
100
50
0
strength development rate
temperature
experimentally determined coefficients

## Slide 32
Mechanisms operative during pressing
Predicting internal conditions
The need to optimize adhesion dynamics
The ABES approach
Adhesion in space and time
Implications
What we will discuss

## Slide 33: Simulated temperature development (here: 28 m continuous MDF press)
Distance from press entry [m]
Cross-sectional position [%]
Temperature [°C]
Mat width: 2.7 m Initial MC (T): 9.6% (26°C)
Target thickness: 20 mm Max. steel belt temperature: 220°C
Target density: 780 kg/m³ Feed speed: 130 mm/s

## Slide 34: Simulated bond strength development (here: 28 m continuous MDF press)
Distance from press entry [m]
Cross-sectional position [%]
Bond strength [MPa]
Mat width: 2.7 m Initial MC (T): 9.6% (26°C)
Target thickness: 20 mm Max. steel belt temperature: 220°C
Target density: 780 kg/m³ Feed speed: 130 mm/s
2
4
6

## Slide 35
Mechanisms operative during pressing
Predicting internal conditions
The need to optimize adhesion dynamics
The ABES approach
Adhesion in space and time
Implications
What we will discuss

## Slide 36
Balance of desitructive and constructive factors upon press exit (or opening):
Destructive versus Constructive
Trapped vapour pressure Strength of bonds
Residual internal stresses Plastic relaxation
Maximise press speed:
2
4
6

## Slide 37: Thermal damage assessment
Up to 265oC (509oF)

## Slide 38: Bond strength maxima and decline
0
2
3
4
5
6
1
100
500
200
400
300
Bond Pressing Time (Sec.)
Bond strength (MPa)
140oC
125oC
110oC
95oC
0
130oC

## Slide 39: Bond strength maxima
0
2
3
4
5
6
1
100
500
200
400
300
Bond Pressing Time (Sec.)
Shear strength (MPa)
140oC
125oC
110oC
95oC
0
130oC
Strength maxima

## Slide 40: Bond strength decline (damage)
0
2
3
4
5
6
1
100
500
200
400
300
Bond Pressing Time (Sec.)
Shear strength (MPa)
140oC
125oC
110oC
95oC
0
130oC
Thermal damage

## Slide 41: Regressed strength development and damage rates versus temperature
Bond Pressing Temperature (oC)
90 100 110 120 130 140
200
150
100
50
0
Isothermal strength
development rates (kPa/sec.)
Isothermal strength
damage rates (kPa/sec.)
strength development rate
strength damage rate
temperature
experimentally determined coefficients
-50

## Slide 42: Simulated temperature development (here: 28 m continuous MDF press)
Distance from press entry [m]
Cross-sectional position [%]
Temperature [°C]
Mat width: 2.7 m Initial MC (T): 9.6% (26°C)
Target thickness: 20 mm Max. steel belt temperature: 220°C
Target density: 780 kg/m³ Feed speed: 130 mm/s

## Slide 43: Simulated bond strength development (showing thermal damage effects at surfaces)
Distance from press entry [m]
Cross-sectional position [%]
Bond strength [MPa]
2
4
6

## Slide 44: Simulated bond strength development (showing thermal damage effects at surfaces)
Distance from press entry [m]
Cross-sectional position [%]
Bond strength [MPa]
2
4
6
Distance from press entry [m]
Cross-sectional position [%]
Bond strength reduction
due to thermal damage

## Slide 45
Rapid cooling of partially cured bonds
to explore Tg as a function of cure level
Cooling gas supply
Cooling gas supply
PTFE cooling blocks

## Slide 46: The cool head

## Slide 47
Cross-sectional position [mm]
Distance from
press entry [m]
Temperature [°C]
Second densification step
Press outlet
Simulation Results
Temperature

## Slide 48: Modelled core bond strength with Tg effects included
0
2
3
4
5
6
1
10
50
20
40
30
Distance from press entry (m)
Bond strength (MPa)
0
Press exit: adiabatic cooling with vapour venting
Δ BS

## Slide 49: Moisture and catalysis effects

## Slide 50: THANK YOU for your attention
Notes: Our Motivation: Understand mechanisms relevant during consolidation of bio-based materials, ...
... like here in a continuous industrial production.
Prozess kurz beschreiben!
Our interest: Physical processes inside the mat.